## Slide 1
The MOS capacitor: what is actually under the probes
gate metal (or poly-Si)
oxide, tox
depletion region
(fixed dopant charge)
W
quasi-neutral bulk (NA or ND)
back ohmic contact
VG
charge balance (Eq. 3, 7)
Gate charge QG = -Qsc
Qsc = space-charge density
in the semiconductor (Eq. 3)
For p-type in depletion:
Qsc = -q NA W < 0
so the gate carries positive charge,
balanced by exposed negative acceptor
ions in the depletion region.
+ + + gate
- - - ionised acceptors
Three terminals in, one number out per bias point: an LCR meter reads Cm and Gm at the gate, and everything in this notebook is inference from that single admittance.

## Slide 2
What the meter reads vs. what you want
meter
Rs
Cox
semiconductor
branch
Cs
Gp
‖
ground /
back contact
measured: Cm, Gm (Eq. 16)
wanted: Gp/ω → Dit (Eq. 17)
Two corrections stand between Cm/Gm and physics:
1. Rs distorts Cm and Gm even in accumulation - extract it from the accumulation plateau (Eq. 19) and undo it (Eq. 20).
2. Cox still sits in series with the semiconductor branch - the admittance transform (Eq. 16) removes it to leave the true Gp/ω.
Skip either step, or use an inaccurate Cox, and the error propagates straight into every Dit you extract.

## Slide 3
Why HF, LF and deep-depletion C-V curves differ
VG
C
Cox
VFB
VT
accumulation
depletion
inversion
LF (equilibrium)
HF (1 MHz)
deep depletion
(swept too fast)
All three agree in accumulation and through depletion; they split only where minority carriers matter - whether they can be supplied fast enough sets which curve you get (Sec. 6).

## Slide 4
The C-V curve's slope is a doping profile
W(V1)
W(V2)
W(V3)
V
1/C²
steeper slope
→ lower N
N(W) = 2 / [qεsA² |d(1/C²)/dV|] (Eq. 12/13)
why |·|, not the bare derivative
The edge of the depletion region is where N(W) is sampled (Eq. 12/13). The textbook sign assumes V rising means more reverse bias; this notebook's VG deepens depletion directly, the opposite sense - N(W) can never be negative, so take the absolute value (Sec. 9).
Sweep V, extract W(V) from C, then N(W) from the local slope of 1/C² - a depth profile built one derivative at a time, well-resolved only where the slope is well-resolved.

## Slide 5
The conductance peak: how a trap dissipates energy
Ec
Ev
EF
Eit - trap level
at the interface
capture / emission,
rate set by τit (Eq. 18)
log ω
Gp/ω
ωτit = 1
single level (Eq. 17)
real (broadened)
A trap only shows up in Gp while it is actively exchanging charge with a band - too slow or too fast relative to ω and it looks capacitive instead, which is why the peak sits at ωτit = 1 and not at higher or lower frequency.

## Slide 6
How this deck works
1 · Edit, then export
Edit any slide in this deck, then export every slide as JPEG
at about 150 dpi (File → Export → JPEG → All slides).
Simpler: run this in the CGV folder - it renders every slide
and copies the JPEGs to both places for you:
./export_figures.sh
2 · Save each JPEG in BOTH folders
Same file name in each. Miss the second one and the website
keeps showing the old picture.
CGV/figures/<name>.jpg
used by the Jupyter notebook
docs/assets/<name>.jpg
used by the documentation website
Slide → file name
Slide 1
fig_cgv_mos_structure.jpg
Slide 2
fig_cgv_equivalent_circuit.jpg
Slide 3
fig_cgv_curve_shapes.jpg
Slide 4
fig_cgv_doping_profile.jpg
Slide 5
fig_cgv_conductance_method.jpg
This .pptx is deliberately not tracked by git - it is your local working copy. The exported .jpg files are what the repository and the website use, so those are the ones to commit.