## Slide 1
Fermi-level alignment and the contact potential difference
A · isolated
Vacuum levels line up.
The Fermi levels do not.
Φp
Φs
Evac
EF
probe
sample
B · connected
Electrons move until the Fermi
levels match. Now Evac does not.
Φp
Φs
Evac
EF
probe
sample
−
−
−
+
+
+
qVCPD
C · nulled
A backing voltage removes the
field, and is what is read.
Φp
Φs
Evac
EF
probe
sample
Vb
CPD = (Φs − Φp) / q = − Vb (null)
Neither work function changes on connection — only the offset between the two vacuum levels, and that offset is the CPD.

## Slide 2
The vibrating capacitor, and where the measurement is made
i(t) = (Vb + CPD) · dC/dt
a DC potential, read as an AC current
probe tip
d1 sin ωt
d0
C(t)
sample
stage
Vb
preamp
Vptp = k (Vb + CPD)
measure away from the null, then extrapolate to it
off-null
window
off-null
window
noise floor
null: Vb = −CPD
Vb
Vptp
The gradient k drifts with spacing, area and gain; the zero crossing does not. So the crossing is the measurement — and it is also where the signal-to-noise ratio is worst.

## Slide 3
A charged dielectric bends the bands of the semiconductor
Positive film charge → accumulation
electrons pile up at the surface; φs > 0
dielectric
space charge
neutral silicon (n-type)
Ec
Ei
Ev
EF
+
+
+
+
Qf
−
−
−
−
Qsc
Dit
qφs
Negative film charge → inversion
holes pile up at the surface; φs < 0
dielectric
space charge
neutral silicon (n-type)
Ec
Ei
Ev
EF
−
−
−
−
Qf
+
+
+
+
Qsc
Dit
qφs
Charge in the film is mirrored by charge in the silicon and in the interface states. Qf + Qsc + Qit = 0 is what fixes φs.

## Slide 4
Light flattens the bands — and the change in CPD is the SPV
Dark
the bands are bent by the film charge
−
−
−
−
Ec
Ei
Ev
EF
qφs
dielectric
n-type silicon
Illuminated
injected carriers screen the charge; the bands flatten
−
−
−
−
Ec
Ei
Ev
EFn
EFp
hν
qφs
dielectric
n-type silicon
SPV = CPDdark − CPDlight = φs(light) − φs(dark)
The probe work function, the calibration and the dielectric term are identical in the two readings, so they cancel. Only the band bending survives.

## Slide 5
A macro-scale Kelvin probe / SPV bench
earthed enclosure (electrical screening + darkness)
vibrating head
d0 ≈ 0.1–1 mm
sample
ref.
reference sample (Au / HOPG),
measured before and after
earthed x–y stage
fibre
control electronics
• vibration drive, ω
• backing voltage Vb
• preamp + off-null fit
• spacing regulation from k
light source
• halogen or LED, shuttered
• intensity swept for saturation
• wavelength swept for Ln
outputs
CPDdark , CPDlight → SPV
Nothing touches the sample. The probe averages over its own diameter, typically 2 mm, so what it reports is an area average.

## Slide 6
How this deck works
1 · Edit, then export
Edit any slide in this deck, then export every slide as JPEG
at about 150 dpi (File → Export → JPEG → All slides).
Simpler: run this in the KPSPV folder — it renders every slide
and copies the JPEGs to both places for you:
./export_figures.sh
2 · Save each JPEG in BOTH folders
Same file name in each. Miss the second one and the website
keeps showing the old picture.
KPSPV/figures/<name>.jpg
used by the Jupyter notebook
docs/assets/<name>.jpg
used by the documentation website
Slide → file name
Slide 1
fig_kpspv_bands_cpd.jpg
Slide 2
fig_kpspv_instrument.jpg
Slide 3
fig_kpspv_surface_bands.jpg
Slide 4
fig_kpspv_spv_bands.jpg
Slide 5
fig_kpspv_setup.jpg
This .pptx is deliberately not tracked by git — it is your local working copy. The exported .jpg files are what the repository and the website use, so those are the ones to commit.