## Slide 1
What a two-probe measurement actually measures
insulating substrate
doped semiconductor layer
metal contact
metal contact
current path
Rm
RC
Rsemi
RC
Rm
measured RT = 2Rm + 2RC + Rsemi
The metal term is negligible; the two contact terms are what TLM is built to isolate.

## Slide 2
The TLM test structure (top view)
isolated doped layer, sheet resistance RS
W
contact width
d
L1
L2
L3
L4
L5
Each neighbouring pair gives one resistance at one spacing. Same sheet, same contacts — only L changes.

## Slide 3
Current crowding and the transfer length
leading edge of the contact
metal contact
doped layer
LT
most of the current has crossed within one transfer length
current still flowing in the semiconductor, I(x)
x = LT
I(x) = I0 exp( –x / LT )
distance into the contact, x
LT = √( ρC / RS ) — lateral transport in the sheet competing with vertical transport across the interface

## Slide 4
Reading four parameters off one straight line
contact spacing, L
total
resistance,
RT
y-intercept = 2RC
x-intercept
= –2LT
slope = RS / W
RT = (RS / W) ( L + 2LT )
slope × W
→
sheet resistance
intercept ÷ 2
→
contact resistance
intercept ÷ 2·slope
→
transfer length
RS × LT2
→
specific contact resistivity
One fit, four numbers — provided the line really is straight.

## Slide 5
Measuring one point: a four-wire sweep on one contact pair
source-measure unit sweeps V, records I
force +
force –
sense +
sense –
contact spacing L
Four-wire probing keeps the lead and probe resistance out of the measured RT — otherwise it lands in the intercept and inflates ρC.
Repeat over every spacing, then fit RT versus L.

## Slide 6
How to update these figures
1 · Edit, then export
Edit any slide in this deck, then export every slide as JPEG
at about 150 dpi (File → Export → JPEG → All slides).
Simpler: run this in the TLM folder — it renders every slide
and copies the JPEGs to both places for you:
./export_figures.sh
2 · Save each JPEG in BOTH folders
Same file name in each. Miss the second one and the website
keeps showing the old picture.
TLM/figures/<name>.jpg
used by the Jupyter notebook
docs/assets/<name>.jpg
used by the documentation website
Slide → file name
Slide 1
fig_tlm_resistance_chain.jpg
Slide 2
fig_tlm_structure.jpg
Slide 3
fig_tlm_crowding.jpg
Slide 4
fig_tlm_plot.jpg
Slide 5
fig_tlm_measurement.jpg
This .pptx is deliberately not tracked by git — it is your local working copy. The exported .jpg files are what the repository and the website use, so those are the ones to commit.